Comparison between ALPOLIC®/fr and ALUCOBOND plus

|  | Items | ALPOLIC®/fr 4 mm | ALUCOBOND plus 4 mm |
| --- | --- | --- | --- |
| 1. (1) (2) | Product composition Skin material Core material | 0.5mm t aluminum (3105-H14) Non-combustible mineral filled core | 0.5mm t aluminum sheets (AA5005, AlMg1, T42) Mineral filled core: |
| 2. (1) (2) (3) | Product dimension Panel thickness Panel size Standard width Standard length Custom (option) width Custom (option) length Product tolerance Thickness Width Length Diagonal difference Bow | 3mm, 4mm, 6mm 965, 1270 & 1575mm 1800 to 7200 mm Available Available ±0.2mm (3-4mm), ±0.3mm (6mm) ±2.0mm ±4.0mm Maximum 5.0 mm Maximum 0.5% of length or width | 3mm, 4mm 1000, 1250 & 1500mm Max. 8000mm Available Available ±0.2mm (3-4mm) -0/+4mm -0+6mm (<4000), -0/+12mm (>4000) unknown unknown |
| 3. (1) (2) (3) (4) (5) (6) (7) | Physical properties Panel weight Thermal expansion Mechanical properties as ACM Rigidity (ExJ) Elongation (ASTM E8) Mechanical properties of skin 0.2% proof stress (ASTM E8) Modules of elasticity Elongation Deflection temperature (ASTM D648) Bond integrity Drum peel (ASTM D1781) Sound transmission loss (STC, ASTM E413) | 7.6 kg/m2 24×10-6/(C 0.21 kNm²/m 5 % > 152 N/mm2 > 70000 N/mm2 > 1% 116(C 123 mmN/mm 27 | 7.6 kg/m2 24×10-6/(C 0.24 kNm²/m unknown > 90 N/mm2 > 70000 N/mm2 > 5% unknown 100 mmN/mm 26 |
| 4. | Fire performance | Refer to Table 1. | Refer to Table 1. |

|  | Items | ALPOLIC®/fr 4 mm | ALUCOBOND plus 4 mm |
| --- | --- | --- | --- |
| 5. (1) (2) (3) (4) (5) (6) | Paint finish Paint material Coating thickness Rust-preventing paint on backside of aluminum skin Coating on reverse side Coating properties 60( gloss Pencil hardness Weather-ability Color retention Gloss retention Chalking Variation of finishes | Lumiflon-based fluorocarbon paint ≥28μ(3/3)—Solid & Metallic Colors Applied (refer to Fig.1 for detail) Polyester coating (refer to Fig.1 for detail) Available in 15-80% H Accelerated test by Weather-O-Meter (WOM) Max. 5 units (4000hrs) Min. 70% (4000hrs) Max. 8 (4000hrs) Fluorocarbon coating: - Solid & Metallic Colors and Stone Timber, Abstract Series Anodised finishes are not available. | PVDF-based fluorocarbon paint, partially Lumiflon-based paint 25μ± 5μ(2-coat/2-bake) Not applied Not applied (mill finish) Available in 30-40% H Outdoor exposure test for 5 years in Florida Max. 5 units Not reported Max. 8 Fluorocarbon coating: - Solid & Metallic Colors - Stone Look Anodised finishes are available. |
| 6. | Panel strength | Equivalent to 3.3mm thick solid aluminum panel | Equivalent to 3.3mm thick solid aluminum panel |
| 7. (1) (2) (3) (4) | Others Minimum bending limit with press brake Traverse Parallel Welding of core material Recycling Warranty | 4 mmt 6 mmt 80 mm R 100 mm R 100 mm R 140 mm R Applicable Can be recycled 20-year finish and panel integrity warranty are available. | Not reported Not reported Not reported Can be recycled Unknown |

Table 1. Summary of Fire Performance Tests

| Category | Country | Test Standard | ALPOLIC/fr | ALUCOBOND plus |
| --- | --- | --- | --- | --- |
| External Cladding | United Kingdom | BS476 Part 7 Part 6 Part 5 | Class 0 Class 1 | Class 0 Class 1 Class P |
|  | Germany | DIN4102 Part 1 | Class B1 | Class B1 |
|  | USA | British Thermal Unit (NFPA 259-93) | Passed <6,000 BTU/sqft | Passed <5,200 BTU/sqft |
|  |  | Climbing Drum Peel Test (ASTM D1781-76) | Passed (>100mmN/mm) | Passed (>100mmN/mm) |
|  |  | Tunnel Test (ASTM E-84) | Class A | Class A |
|  |  | Modified ASTM E-108 | Passed | Passed |
|  |  | UBC 26-9 & NFPA 285, ISMA Test (Intermediate Scale Multi-story Apparatus) | Passed | Not reported |
|  | Canada | CAN/ULC-S 134-92, Full-scale Exterior Wall Fire Test | Passed | Not reported |
|  | China | GB8625, GB8626 & GB8627 | Class B1 | Class B1 (unknown) |
|  | Japan | Heat Release Test for Non-combustible Material | Passed | Not reported |
| Roof | USA | Fire Test for Roof Covering (ASTM E108) | Passed Class A | Not reported |
| Fire Resistant Rating Wall | USA | 1-hr Fire Rating and 2-hr Fire Rating (ASTM E119) | Does not impair fire resistant rating wall | Not reported |
| Interior | USA | Interior Room Corner Test (UBC 26-3) | Passed | Not reported |
|  | USA | Combustion Toxicity Test, New York State Uniform Fire Prevention and Building Code | Passed | Passed |

Table 2. Comparison of Heat Release Vale of Core Materials by In-house Lab Test Data

| Type of ACM | ALPOLIC/fr | ALUCOBOND plus |
| --- | --- | --- |
| Polymer content of the core (wt %) | 30 | 30 |
| Hydroxy-filler of the core (wt %) | 70 | 70 |
| Type of resin | LLDPE | unknown |
| Type of Hydroxy-filler | Aluminum Hydroxide | Aluminum Hydroxide + Calcium Carbonate (*1) |
| Heat potential of the core (MJ/kg) | 12.6 | 13.3 |
| Specific gravity of core | 1.63 | 1.67 |
| Heat potential as a panel MJ/sqm (as 3.0mm core) | 61.6 | 66.6 (*2) |

Note: (*1) Aluminum hydroxide starts decomposing by heat around 190 degree C, and it generates water by reaction.  Calcium carbonate does around 900 degree C.  Resin's burning temperature is around 400-550 degree C, therefore, calcium carbonate will not work well as an extinguishing element in case of fire.  Calcium carbonate should be regarded as a filler just to increase its volume.

(*2) Lower heat potential means lower fire spread would be expected in case of fire.

## Fig. 1 Major Difference in Composition Details

|  | ALPOLIC/fr | ALUCOBOND plus |
| --- | --- | --- |
| Paint finish | Lumiflon-based fluorocarbon ≥28mic (3/3) | PVDF-based fluorocarbon 25±5mic (2/2) |
| Rust-preventing paint | Applied | None |
| Service coating | Polyester coating | None (mill finish) |

# Text boxes

Rust-preventing paint

Aluminum skin

Paint finish

Aluminum skin

Rust-preventing paint

Non-combustible mineral filled core

Service coating